CHAOS INCORPORATED

Design System for Renn

STARLINK ONE

Technical Design & Manufacturing Package

Heart-Cut Emerald Ring · Sterling Silver · Chain-Link Motif

Document Type: Full Technical Specification, Tech Pack, Manufacturing Brief (EN/中文), CAD Requirements & QC Checklist

Revision: 1.0 (Draft — Chain-Link Motif Pending Reference Images)

Date: 14 July 2026

Prepared by: Technical Design — Chaos Incorporated

# 1. Project Overview

Starlink One is a signature engagement/statement ring in the Renn design system: a heart-shaped natural emerald center stone in a secure 4-prong setting, flanked by a chain-link / infinity motif on both shoulders, executed in full 925 sterling silver with an initial high-polish finish that is intentionally left unprotected to allow natural tarnish and patina to develop with wear.

### 1.1 Design Intent

- Center stone reads as the visual anchor: vivid green, brilliant-faceted heart, set high enough to catch light from the side without being fragile.

- Chain-link/infinity motif on the shoulders is the signature element of the piece — it must be treated as a precision-matched pair (mirrored left/right), not a generic decorative filler.

- Finish is deliberately "alive": no rhodium, no anti-tarnish lacquer. The metal is expected to oxidize and patina over time — this is a design feature, not a defect, and must be communicated to the factory so it is not treated as a QC failure.

### 1.2 Governing Source of Truth

Four client reference images define the exact chain-link/infinity geometry and are the single source of truth for that motif. This package was generated before those images were available in this session — Section 6 (Chain-Link / Infinity Motif Specification) is structured as a fill-in template pending upload, and CAD/manufacturing work on the motif should not proceed to tooling until Section 6 is finalized against the reference images.

# 2. Technical Specifications

| Parameter | Specification | Tolerance |
| --- | --- | --- |
| Ring size | US 7 — inner diameter 17.3 mm | ±0.1 mm |
| Inner circumference (derived) | 54.35 mm (π × 17.3 mm) | ±0.3 mm |
| Base material | 925 Sterling Silver (92.5% Ag / 7.5% Cu alloy) | Assay ≥92.5% Ag |
| Plating / coating | None — bare polished silver, patina intended | N/A |
| Center stone | Natural emerald, heart shape, brilliant cut, vivid green | See Section 4 |
| Center stone size | 8.0–9.0 mm (length ≈ width) | ±0.2 mm |
| Setting type | 4-prong, open gallery | See Section 5 |
| Signature motif | Chain-link / infinity, both shoulders, mirrored | See Section 6 |
| Finish | High polish (mirror), hand-buffed, no matte zones | Class-A jewelry polish |
| Hallmark | "925" stamp + Chaos Incorporated maker's mark, interior shank | Legible at 10x |

# 3. Detailed Tech Pack

All dimensions below are measured on the physical horizontal/vertical axes of the ring as worn (shank on finger, stone facing up). Values marked "Notes" carry construction intent so the factory does not need to infer designer intent.

| Dimension | Value | Tolerance | Notes |
| --- | --- | --- | --- |
| Inner diameter (ring size) | 17.3 mm | ±0.1 mm | Measured post-cast and post-polish, not pre-sizing |
| Shank width — back/base (narrowest point) | 1.8 mm | ±0.1 mm | Comfort-fit half-round exterior, flat interior |
| Shank thickness (metal depth, base) | 1.5 mm | ±0.1 mm | Full 925 silver, no hollow core in shank |
| Shank width — at shoulder (motif transition) | 2.2–2.4 mm | ±0.15 mm | Widens gradually into motif, no hard step/seam |
| Shoulder / motif zone width (per side) | 3.5–4.0 mm | Per ref. images (Sec. 6) | Final value locked once reference images are reviewed |
| Gallery / basket height (girdle to shank rail) | 4.5–5.5 mm | ±0.2 mm | Open basket to let light through pavilion |
| Prong base diameter | 1.2 mm | ±0.05 mm | Round, tapering toward tip |
| Prong tip diameter (post-finishing) | 0.8 mm | ±0.05 mm | Hand-filed/polished by setter after stone-setting |
| Prong height above girdle | 1.0–1.2 mm | ±0.1 mm | Enough coverage for security without hiding crown facets |
| Seat depth (girdle bearing surface) | 0.3–0.5 mm | ±0.05 mm | Cut to match heart-brilliant pavilion angle |
| Estimated total ring height off-finger (crown to base) | 9.5–11.0 mm | ±0.3 mm | Sum of basket + stone depth + prong clearance |
| Estimated finished weight (silver only, stone excl.) | 3.8–4.6 g | ±0.3 g | To be confirmed by CAD mass properties before casting |

⚠ PENDING / FLAGGED FOR CLIENT CONFIRMATION: Shoulder/motif width, shank taper curve, and overall silhouette in the shoulder zone are designer defaults based on stone size and standard shoulder engineering. These must be re-validated once the four reference images are reviewed, since the chain-link motif's own width/pitch may force a different shoulder profile.

# 4. Gemstone Specification

| Attribute | Specification |
| --- | --- |
| Species / variety | Natural emerald (beryl), no synthetic or lab-grown substitute |
| Shape | Heart |
| Cut style | Brilliant (heart-brilliant faceting) |
| Dimensions | 8.0–9.0 mm length × 8.0–9.0 mm width (near-symmetrical heart, L:W ≈ 0.95–1.05:1) |
| Estimated depth | 5.0–5.8 mm (≈65% of average width, typical heart-brilliant proportion) |
| Estimated carat weight | ≈2.0–2.6 ct (formula estimate: L × W × D × 0.0090; confirm on physical stone at sourcing) |
| Color | Vivid green, medium-dark tone, high saturation — no strong secondary blue/yellow modifier preferred |
| Clarity | Eye-clean face-up preferred; minor-to-moderate jardin (internal inclusions) is acceptable and expected in natural emerald — must be disclosed on the gem cert, not treated as a defect |
| Treatment disclosure | Standard oil treatment (traditional cedarwood oil, minor/moderate per CIBJO/GIA convention) expected and must be disclosed in writing; no resin/polymer fracture-filling |
| Orientation in setting | Point of heart oriented toward the base of the finger (toward the palm) unless client specifies point-up |
| Certification required | Independent gemological report (GIA, AGL, or equivalent) confirming natural origin, treatment, and dimensions prior to setting |

### 4.1 Durability Note (flag for client awareness)

Emerald is significantly softer and more brittle than diamond or sapphire (Mohs 7.5–8 but with high inclusion density and low toughness), and heart shapes concentrate stress at two points: the center cleft (V-notch) and the bottom tip. This design's prong layout (Section 5) places a prong at both of those exact points deliberately, and the piece should be marketed/cared-for as a stone requiring the same care as other emerald jewelry (avoid impact, avoid ultrasonic cleaning, avoid steam cleaning).

# 5. Setting & Prong Specification

### 5.1 Prong Layout (4-prong, heart-specific placement)

- Prong 1 — Point prong: centered on the bottom tip (V-point) of the heart. This is the single most vulnerable point on the stone and must fully cradle the tip, not just touch it.

- Prong 2 — Cleft prong: centered on the top cleft (V-notch). Recommend a split/notched "V-prong" tip profile so the prong hugs both facet planes of the cleft rather than resting on a single point.

- Prong 3 & 4 — Shoulder prongs: positioned at the widest point of each heart lobe (left and right rounded shoulders of the heart), symmetric about the centerline.

### 5.2 Prong Construction

| Feature | Spec |
| --- | --- |
| Prong profile | Round, tapering claw — no faceted/square prongs |
| Base diameter | 1.2 mm (±0.05 mm) |
| Tip diameter after finishing | 0.8 mm (±0.05 mm) |
| Tip shape | Rounded bead tip (snag-free) — cleft prong (Prong 2) is split/notched per 5.1 |
| Metal coverage over crown/girdle | 0.6–0.8 mm per prong, enough to lock the girdle without covering table-facing facets |
| Prong-to-gallery attachment | Cast integral to basket — no soldered-on prongs |

### 5.3 Gallery / Basket

- Open 4-rail basket (one rail feeding each prong) to allow light transmission through the pavilion — supports "brilliant cut" visual intent.

- Basket wire gauge: 1.0 mm round, matched to shank metal for uniform patina.

- Seat cut to the exact pavilion angle of the approved heart-brilliant stone — seat must be re-cut in CAD after the physical stone's actual depth % is confirmed (Section 4).

# 6. Chain-Link / Infinity Motif Specification

⚠ PENDING / FLAGGED FOR CLIENT CONFIRMATION: This entire section is a fill-in template. No reference images were available when this package was generated. Do not release Section 6 to CAD/tooling until every field below is completed against the four client reference images.

### 6.1 Fields to Confirm Against Reference Images

| Field | To be confirmed |
| --- | --- |
| Motif type | Static sculptural chain-link vs. articulated/moving links vs. infinity-loop (figure-8) vs. hybrid — CONFIRM |
| Link count per shoulder | TBD from images |
| Link shape | Oval / round / elongated — TBD |
| Link internal opening (visible "hole") | TBD — affects castability, min. recommended 0.8 mm clear opening |
| Wire gauge of each link | TBD — recommend 1.0–1.4 mm round or half-round for structural strength in cast silver |
| Link pitch / overlap spacing | TBD |
| Orientation (links flat vs. links twisted 90° at intervals, true-chain style) | TBD |
| Symmetry rule | Left shoulder must mirror right shoulder exactly (not rotationally identical — true mirror image) |
| Transition into shank | TBD — whether motif fades into plain shank or terminates abruptly at a collar |
| Transition into basket/gallery | TBD — how top-most link meets the prong basket |

### 6.2 Structural / Manufacturing Decision Required

Two fundamentally different builds are possible and must be decided before CAD starts, since they change tolerances, printing method, and cost:

- Option A — Cast solid motif (recommended default): links are modeled and cast as one fused piece with the shank/basket. Visually reads as chain-link but does not move. Stronger, cheaper, standard for this kind of ring.

- Option B — Articulated/functional links: links are cast or fabricated separately and mechanically joined so they move. Adds significant cost, fragility, and assembly steps; typically reserved for pieces where the chain motion itself is the point (e.g., a bracelet).

Recommendation: Option A, unless the reference images clearly show the links must swing/rotate independently — flag to client for explicit sign-off either way.

# 7. Shank & Band Specification

| Feature | Spec |
| --- | --- |
| Profile (exterior) | Half-round / D-profile |
| Profile (interior) | Flat, lightly rounded edges (comfort-fit) for all-day wear |
| Inner diameter | 17.3 mm ±0.1 mm (US 7) |
| Width at base (6 o'clock, narrowest) | 1.8 mm ±0.1 mm |
| Width at shoulder (12 o'clock approach) | 2.2–2.4 mm ±0.15 mm, widening to meet motif |
| Thickness (metal depth) at base | 1.5 mm ±0.1 mm |
| Sizing allowance | Design and cast at exact target size; do not rely on post-cast stretching to hit size — stretching after the motif is cast risks distorting the chain-link pattern |

# 8. Finish & Surface Treatment Specification

| Stage | Requirement |
| --- | --- |
| Initial finish | High polish / mirror finish, Class-A jewelry standard, all surfaces including motif undercuts |
| Plating | None. Do not rhodium-plate. Do not apply e-coat or protective lacquer. |
| Patina | Natural tarnish and oxidation over time is an intended design outcome — factory QC must not reject product for "lack of anti-tarnish treatment" |
| Hallmark | "925" stamped on interior shank, plus Chaos Incorporated maker's mark, both legible at 10x magnification, stamped before final polish so edges are clean |
| Cleaning before ship | Ultrasonic cleaning of metal only permitted before stone-setting; after the emerald is set, hand-clean only (steam and ultrasonic can damage oiled emerald) |
| Packaging finish check | Ring shipped with a light protective film or bag to avoid scratching during transit; no anti-tarnish strips inside the box (would work against intended patina) |

# 9. Manufacturing Brief — English

### Project

Starlink One — heart-cut emerald ring, 925 sterling silver, chain-link/infinity shoulder motif. Client: Renn / Chaos Incorporated.

### To the Factory

Please read this brief in full before quoting or starting CAD. This piece has two non-negotiable requirements that differ from a standard ring order: (1) the finish must NOT be rhodium-plated or lacquer-coated — the metal is meant to tarnish naturally over time, and (2) the shoulder chain-link motif must match the client's four reference images exactly in link count, shape, and proportion, not a generic "chain pattern." Reference images will be supplied separately/appended; if they are missing from your packet, stop and request them before modeling.

### Materials

- Metal: 925 sterling silver throughout (shank, gallery, prongs, and motif) — no base-metal core, no plating.

- Center stone: natural heart-shaped brilliant-cut emerald, vivid green, 8–9 mm, supplied with independent gemological certification (GIA/AGL or equivalent). Stone will be supplied by client/sourcing partner unless otherwise agreed — confirm supply chain before quoting stone-setting labor only vs. stone + setting.

### Construction

- Ring size US 7 — finished inner diameter 17.3 mm ±0.1 mm, measured after casting, polishing, and stone-setting (not before).

- 4-prong setting, prong placement locked to the heart's point, cleft, and two shoulders (see Section 5 of the full tech pack) — this is not a generic 4-prong layout and must not be substituted with an evenly-spaced 4-prong pattern.

- Chain-link/infinity motif cast integral to the piece (no soldered-on links) unless the reference images explicitly call for articulated/moving links — if in doubt, ask before committing to tooling.

### Finish

- High polish / mirror finish on all surfaces, including motif undercuts — no matte or satin zones.

- No rhodium plating. No anti-tarnish coating, lacquer, or e-coat of any kind.

- "925" hallmark plus Chaos Incorporated maker's mark stamped on interior shank, legible at 10x, stamped before final polish.

### Handling

- After stone-setting: hand-clean only. No ultrasonic or steam cleaning once the emerald is in place (oil-treated emerald can be damaged by both).

- Ship with light protective wrap only — do not include anti-tarnish paper/strips in packaging, as this works against the intended patina.

### Approval Gate

A resin/wax 3D print of the full CAD model (stone-in-place, to scale) must be sent for client sign-off before metal casting begins. Do not proceed to casting on CAD approval alone.

# 10. 制造工艺说明书（简体中文技术版）

### 项目名称

Starlink One（星链一号）—— 心形祖母绿戒指，925纯银材质，双肩链条/无限符号纹样。客户：Renn / Chaos Incorporated（混沌股份）。

### 致工厂说明

请在报价或开始建模前完整阅读本说明书。本产品有两项与常规订单不同的强制性要求，不可协商：（1）成品表面禁止镀铑、禁止上光油或任何防氧化涂层——银材需要随佩戴自然氧化、产生包浆，这是设计效果的一部分；（2）戒指双肩的链条/无限符号纹样必须与客户提供的四张参考图片完全一致（包括链节数量、形状与比例），不可使用通用链条纹样替代。参考图片将单独提供或随附件发送；若您收到的资料中缺少参考图片，请在建模前暂停并索取，切勿自行推测纹样设计。

### 材质要求

- 金属材质：戒圈、爪镶篮、爪齿及链条纹样全部使用925纯银（含银量92.5%），不得使用贱金属芯材，成品不得电镀。

- 主石：天然心形明亮式切割祖母绿，鲜绿色，尺寸8–9毫米，须附独立宝石鉴定证书（GIA、AGL或同等资质机构出具）。除另有约定外，主石由客户/寻石方提供——报价前请与客户确认是仅报镶嵌工费，还是包含主石采购。

### 结构与尺寸

- 戒指尺寸：美码7号——成品内径17.3毫米，公差±0.1毫米，须在铸造、抛光及镶石全部完成后测量，而非铸造前的蜡型尺寸。

- 镶嵌方式：四爪镶嵌，爪位须严格对应心形宝石的底部尖端、顶部凹口（心形缺口）及左右两侧肩部（详见完整技术包第5节），此为针对心形宝石的专用爪位设计，不可替换为常规四爪均匀分布方案。

- 链条/无限符号纹样须与戒身、爪镶篮一体铸造成型，不允许后期焊接拼装链节；若参考图片明确要求链节可活动（真实链条结构），须在开模前与客户书面确认，不可自行判断。

### 表面处理

- 全器表面（含纹样凹陷处）均须抛光至镜面高抛光效果，不得留有哑光或磨砂区域。

- 禁止镀铑，禁止使用任何防氧化涂层、封层或电镀处理。

- 须在戒圈内侧打印“925”纯度印记及Chaos Incorporated品牌印记，印记须在10倍放大镜下清晰可辨，并在最终抛光前完成打印，以确保印记边缘整洁。

### 镶石后处理规范

- 主石镶嵌完成后，仅可手工清洁，严禁使用超声波或蒸汽清洗——祖母绿通常经过注油处理，超声波及蒸汽清洗均可能对宝石造成损伤（裂纹扩大或注油流失）。

- 包装时仅可使用轻质保护包裹材料，禁止在包装内放置防氧化纸或防氧化条，因其效果与本设计要求的自然包浆效果相悖。

### 确认节点（重要）

金属铸造前，须先提供按实际比例、含仿真主石的树脂或蜡质3D打印样品，交由客户确认签字后方可进入铸造环节。仅凭CAD电子图纸批准不可直接进入铸造工序。

# 11. CAD Requirements

### 11.1 Software & File Formats

| Deliverable | Format | Notes |
| --- | --- | --- |
| Native CAD model | .3dm (Rhino) or Matrix/RhinoGold native | Fully parametric where possible, especially motif links |
| Print-ready mesh | .stl | Min. 0.01 mm resolution, watertight, no non-manifold geometry |
| Engineering reference | .stp / .step | For factory tooling reference and archive |
| 2D dimensioned drawing | .pdf + native vector | Front, side, top, and section views with all Section 3 dimensions called out |
| Renders | .png/.jpg, min. 3000px | Front, 3/4, side, top-down, and one exploded-view render of prong+basket+shank construction |

### 11.2 Modeling Requirements

- Model the stone as an accurate proxy (correct heart-brilliant facet geometry at 8–9 mm) so the seat/prongs are engineered against real geometry, not a placeholder sphere/box.

- Chain-link/infinity motif must be modeled from the four reference images at 1:1 scale reference overlay — do not approximate by eye.

- Minimum wall thickness anywhere in the cast structure: 0.8 mm (castability floor for 925 silver investment casting).

- All undercuts in the motif must include adequate draft/relief for investment mold release — flag any link geometry that fully encloses a void (true interlocking rings) since those cannot be cast as one piece and require the Section 6.2 articulated-link decision.

- Model at the exact target ring size (17.3 mm ID) — do not rely on post-cast sizing to hit tolerance, since sizing after the fact can distort the motif.

### 11.3 Tolerances

| Parameter | CAD tolerance |
| --- | --- |
| Overall dimensions | ±0.1 mm |
| Ring inner diameter | ±0.1 mm (hard requirement, matches finished-piece spec) |
| Prong tip geometry | Model to +0.1 mm oversize — final tip shaping is done by hand by the stone-setter after casting |
| Motif link geometry | ±0.05 mm per link, consistent across all links on one shoulder |

### 11.4 Validation Gate

A physical resin or wax print at 1:1 scale, with a stone proxy in place, must be produced and approved by the client before any metal is cast. This is the primary check for fit, proportion, and motif accuracy against the reference images.

# 12. Quality Control Checklist

To be completed by factory QC before shipment, and independently spot-checked by client-side QC on receipt.

| # | Category | Check | Pass/Fail |
| --- | --- | --- | --- |
| 1 | Material | XRF assay confirms ≥92.5% silver content |  |
| 2 | Ring size | Inner diameter gauge check reads 17.3 mm ±0.1 mm |  |
| 3 | Weight | Finished weight within ±0.3 g of approved CAD mass properties |  |
| 4 | Stone security | Push-test on all 4 prongs individually — zero stone movement or rocking |  |
| 5 | Stone orientation | Heart point aligned to shank centerline per Section 4 spec |  |
| 6 | Motif symmetry | Left and right shoulder motifs are true mirror images — check against master CAD render, not "close enough by eye" |  |
| 7 | Motif accuracy | Link count, shape, and pitch match approved reference-image spec (Section 6) |  |
| 8 | Surface finish | Full mirror polish, no visible casting porosity, no fire scale, no tool/file marks, undercuts of motif fully polished |  |
| 9 | Prong finishing | No sharp/snag edges on any prong tip; cleft prong (Prong 2) correctly notched/split |  |
| 10 | Prong coverage | Each prong covers girdle by 0.6–0.8 mm without obscuring crown facets |  |
| 11 | Hallmark | "925" + maker's mark present, legible at 10x, correctly positioned on interior shank |  |
| 12 | Stone quality | No visible chips or cracks, especially at the cleft and point (highest-risk zones); inclusions consistent with certified clarity grade |  |
| 13 | Cleanliness | No polishing compound residue in motif undercuts or under prongs — check under 10x loupe |  |
| 14 | No unauthorized finish | Confirm NO rhodium plating, NO anti-tarnish coating was applied |  |
| 15 | Certification | Gemological report accompanies stone; matches stone actually set (cross-check measurements) |  |
| 16 | Packaging | Ring box + gem certificate included; no anti-tarnish strips in packaging |  |

# 13. Sign-Off / Approval

| Role | Name | Signature | Date |
| --- | --- | --- | --- |
| Designer (Chaos Incorporated) |  |  |  |
| Factory Representative |  |  |  |
| Client (Renn) |  |  |  |

⚠ PENDING / FLAGGED FOR CLIENT CONFIRMATION: This document is Revision 1.0 and is not final. Section 6 (Chain-Link / Infinity Motif) must be completed against the four client reference images, and Section 11.4's physical print must be approved, before this design proceeds to metal casting.